TPU产品物性表Table of Physical Properties
1、 名称: LS-1005 聚酯型热塑性聚氨酯

Name: LS-1005 polyester thermoplastic polyurethane

2、 外观: 透明或有色卷形薄膜或片

	检测项目

Item(s)
	测试标准

Test method
	单位

Unit
	典型值

Typical Value

	硬度

Shore Hardness
	ASTM D2240
	Shore A
	95

	比重

Specific Gravity
	ASTM D792
	g/cm3
	1.22

	拉伸强度

Tensile strength
	ASTM D412
	MPa
	45

	极限延伸率

Ultimate Elongation
	ASTM D412
	%
	600

	100%模量
Tensile Stress at 100% Elongation
	ASTM D412
	MPa
	16

	撕裂强度

Tear Strength
	ASTM D624
	KN/m
	150

	耐高低温

Temp Resistance
	/
	ºC
	-30~120

	熔点

Melting point
	/
	ºC
	155~165


Appearance: transparent or colored rolled film or sheet

3、 产品物性参数

Physical properties of the product

测试样品规格：0.5mm；23℃,

Test sample specification：0.5mm,23 ℃
典型值：

除非另有说明，所提供数值均为室温下标准测试样本测得的典型值。这些数据应仅视为指导性参考值，不可作为具有约束力的材料规范或保证性能指标。
Typical values ：
Unless specified to the contrary, the values given are typical values which have been established on standardized test specimens at room temperature. The figures should be regarded as guide 
values only and not as binding material specification or warranted properties.
